## Slide 1: Dynamical Decoupling of Nitrogen-Vacancy Electron Spins in Diamond and Nanodiamond
Defense of the Bachelor thesis
by Richard Kullmann
26.02.2017

## Slide 2: Contents
Motivation
Theory
Setup
Measurements
Conclusion and Outlook

## Slide 3: Motivation
magnetic field imaging: idea of single spins as sensors on the nanoscale
quantum system used for this purpose ideally meets these criteria:
  stable
  controllable
  can be easily prepared and read out

## Slide 4: Motivation
NV center meets these conditions
High sensitivity requires long coherence times
NV spin has to be decoupled from unwanted interactions with the environment
Dynamical decoupling techniques

## Slide 5: NV center
Vacancy (V) next to substitu-
tional nitrogen (N) atom in
diamond lattice
optically stable
long coherence times even
at room temperature
single photon fluorescence
Theory

## Slide 6: NV center
description with 3 level system
GS mS=0 and mS=±1 separated by D=2.87 GHz
relaxation ES→GS:
luminescence with ZPL
at 637nm
highest fluorescence
at mS=0
optical initialization
NV Hamiltonian:
Theory

## Slide 7: Rabi oscillations
single electronic spin (2 level system) in B-field → Zeeman splitting:
adding oscillating field
→
Theory

## Slide 8: Rabi oscillations
Theory
total Hamiltonian:
for ω1<< ωB, perturbation theory yields:
Rabi’s formula
in resonance: ω=ω10 →

## Slide 9: Bloch sphere
Image of rotations on bloch sphere
Theory

## Slide 10: Dynamical Decoupling sequences
Hahn Echo
  1st spin echo experiment
  Measurement of T2
Theory

## Slide 11: Dynamical Decoupling sequences
CPMG
  multiple π rotations around single axis
  higher decoupling efficiency than Hahn Echo
Theory

## Slide 12: Dynamical Decoupling sequences
XY
  CPMG pulse spacing
  π rotations around 2 axes → 3D decoupling
Theory

## Slide 13: Spectral decomposition
In general: loss of coherence obeys C(t)=e-Χ(t)
with
S(ω): spectral density function
F(ωt): filter function
Theory

## Slide 14: Setup

## Slide 15
Measurements

## Slide 16: Conclusion and Outlook
successful implementation of DD protocols
CPMG: improvement of factor 50 in nanodiamond and 200 in bulk → 60 μs
CPMG outperforms XY
Spectral density in good agreement with other experiments
error sources: BPG (pulse errors), MW splitter, AOM
future
  better time and phase control
  Implementation of other decoupling protocols